JSC "A.S.Yakovlev Design Bureau"

125315, Moscow, Leningradsky prospect, 68                Teletype: 611486 "PLAZ"

Tel.: 8 (499) 158 3667 Fax: 8 (495) 151 5771                E-mail: okb@yak.ru

4/4/2011					                 To № ___________________________

№ 01-1022/1252				                from_____________________________

To operating and overhaul agencies,                       
owners of Yak-52 Aircrafts

YAK 52 Aircraft continuing airworthiness, 
in connection with the crash of Yak-52 N 9010607
Ekaterinburg’s Aviation Sports Club

Voluntary Association for Assistance to Army,

Air Force and Navy

Crash investigations of Yak-52 serial number 9010607 Ekaterinburg’s Aviation Sports Club Voluntary Association for Assistance to Army, Air Force and Navy of Russian Federation are found the destruction of the elevator sector 525100-80.

The research found that the cause of the sector 525100-80 destruction is combination of high level dynamic loading of the sector under actual operating conditions and manufacturing defects:
- manufacturing the sectors of the plate instead of forging (forged);
- manufacturing the sectors from the AK-4 instead of the AK-6;
- underestimating of fillet radius (transition to thickening of the sector) during the production process (deviations from the drawing requirements);
- large surface roughness in the fillet area ​;
- negative (parallel to the fillet) location of the structure of sector’s material.

Decide to produce the sectors of the elevator from the steel 30ХГСА instead of the AK-6 alloy and issue the bulletin of their replacement in service, in connection with design-manufacturing trouble in the sectors 525100-80, which directly affect the operational safety of A.S.Yakovlev Design Bureau’s aircrafts Yak-52.

To perform dismantling and inspection of the sectors 525100-80 for absence of cracks in the fillet area and upper mounting holes in the flanges of the elevator using capillary method ЦM15-B or ЦM16-B in accordance with  Industrial Standard (OST) 1 90282-79 “Product Quality. Non-Destructive Testing. Capillary methods”  after paint-and-lacquer coating removal in places of inspection; in addition to the instructions of aircraft inspection of 200-hour maintenance check and inspection of the sectors 525100-80 for absence of cracks using visual-optical method (DB Ref. No. 01-1022/4011 from 25.11.2010) on all operated Yak-52 aircrafts.

Inspection must be performed by certified experts by filling out the record and registration in the elevator certificate.

If cracks and other inadmissible damages are detected, perform replacement of the sector, record the place of damage and inform the bureau.

Inspection must be performed every 25 ± 5 hours of flying using capillary method until the sector 525100-80 of AK alloy will be replaced with steel.

CHIEF DESIGNER 
JSC "A.S.Yakovlev Design Bureau"       /signed/                               D.K.DRACH

APPROVED                                                                     APPROVED 
Commander of military unit                                              Chief Designer
44777-A                                                                            JSC "A.S.Yakovlev Design Bureau"

/signed/.... N. MARCHENKO                                        /signed/............. D. DRACH                                                 
April 12, 2011                                                                April 12, 2011

AGREED 
Chief Engineer

Department of Aviation of Voluntary Association

for Assistance to Army, Air Force and Navy 
/signed/............. E.UGOLNIKOV
April 14, 2011

DECISION № Б-46/52-11

to issue of the bulletin of Yak-52 aircrafts modifications

1. Subject: Aircraft’s elevator control. Replacing the AK-6 with steel 30ХГСА in the elevator 525100-80-3 sector’s construction.     
2. Reason for Issuance: Disastrous fatigue failure of the sectors 525100-80-3 made of the AK-6 as a result of high level dynamic loading in continuous exploitation.

3. Brief description of modifying, the number of materials necessary for one aircraft modification, graphic engineering tasks, etc.: Manufacture the sector of the elevator 525100-80 from the steel 30ХГСА. Material required: 
- sector 525100-80-3, made of steel 30ХГСА – one;
- bearing ОУ1008 - one;
- bracket 525100-81-1 - one;
- bracket 525100-81-2 - one;
- bolt 3189A-4-6 - eight.

4. The changes implemented in the series № - not implemented. Notice № - not issued.
5. Aircrafts entitled to modification according to the bulletin: The elevators - in all types of Yak-52 aircrafts after the bulletin enter into force.

6. Bulletin assigned code: БД.

7. Aircraft’s developer sends technical information to the supplier of modifying sector for the Bulletin development: Enterprise JSC "Shakhtinsky aircraft repair plant Russian Defence Sports and Techniques Organization" Ltd. has been provided by: the drawing of the Sector 525100-80 and the drawing of the Sector 525100-80-3. JSC "Shakhtinsky aircraft repair plant Russian Defence Sports and Techniques Organization" Ltd. has to complete the Bulletin development in the following amount:
- manufacture the sector 525100-80-3 from the steel 30ХГСА;
- perform dismantling of bearing and brackets 525100-81–1, 525100-80-2 from the old sector;
- fulfil the assembly of a new sector 525100-80 with bearing and brackets 525100-81-1, 525100-80-2  installation (in the absence of damage use the old);
- prove the technology of mounting of the sector 525100-80 and balancing weight on the elevator;
- balance the elevator according to the instructions on the balance and determine necessity for its carrying out in the case of sector’s replacement in service.

8. Bulletin’s developer: Enterprise JSC "Shakhtinsky aircraft repair plant Russian Defence Sports and Techniques Organization" Ltd. has to develop the Bulletin within one month after receiving Decision.

9. To be performed by: JSC "Shakhtinsky aircraft repair plant Russian Defence Sports and Techniques Organization" Ltd.  
10. The condition of modifications: Perform the replacement of the sectors as far as operators supply elevators at JSC "Shakhtinsky aircraft repair plant Russian Defence Sports and Techniques Organization" Ltd. and during the next heavy overhaul of the aircrafts.

11. Modifications beginning: After the bulletin enter into force.
12. Modifications finishing: in May 2012.
13. The order and delivery time (graphic engineering tasks): Not required.
14. For aircrafts operated abroad: Issue the bulletin.
15. Necessity for specification of operations documentation: Update Technical description, Service instruction and Maintenance program of Yak-52 aircraft.

16. Costs to be covered by: Operator.

Department head of
Military Unit 44777-A
«….» ………......... 2011

Deputy Chief Designer of

JSC "A.S.Yakovlev Design Bureau"
/signed/.............. B. POPKOV
«….» ……..…....... 2011

Chief of 371 military representative office Ministry of Defence 
 /signed/............. A. VERIGIN
«….» ……..…....... 2011