ArmorShield Plus InterceptTM Description
ArmorShield Plus InterceptTM (AS+ITM) is a new shrinkwrap material used for making pre-formed, heat shrinkable protective covers.  AS+I has anti-corrosive properties, offering a stronger cover with water wicking properties and a corrosive gas barrier and removal system.  AS+I is composed of five layers and is used in making heat-shrinkable protective kits, and serves to prevent corrosion of stored or shipped items.
[image: image1.jpg]



            CH-47D Shrinkwrap Kit
The two outer layers are a white, special shrink/stretch polyethylene film, which remains flexible after shrinking and contains an advanced ultra-violet inhibitor to protect the film for a long period of time.
The third layer is co-extruded with the first two and contains Static Intercept Technology resin, which blocks corrosive gases that have migrated through the first two layers.  It will not, however, scavenge corrosive gases already trapped within the packaging because the Intercept layer is isolated from the gases by the thermoplastic bonding layer.
The fourth layer is a 1.5-mil thermoplastic bonding plastic containing no solvents, which is applied to the film in a hot continuous layer.  This layer does not come in contact with the surface of the item being protected and will not leave a residue on the surface.  Its primary function is to bind the shrinkfilm and polyester fabric together.
The fifth, and inner layer, is a unique spun non-woven polyester fabric.  It will not react with the finish or react with any residual solvents in the finish.  It is hydrophilic which is anti-condensing and anti-fogging but which wicks away moisture.  In addition, it allows the curing process to continue.  The anti-condensing properties of this layer help protect the finish from moisture damage.  The polyester fabric is coated with Corrosion Intercept Ink, which uses bound copper to sacrificially remove corrosive gases trapped within the envelope and inhibit mold and mildew that might try to form within the cover.  The fifth layer also reflects a majority of the heat during the shrinking process, protecting the finish from over heating and actually causes the film to shrink faster.   The heating process will only temporarily increase the equipment skin temperature 34-50 degrees Fahrenheit over ambient temperature.  The inner non-woven layer is engineered for total scratch resistance, maximum cushion, softness and abrasion resistance.  

When shrunk, all layers shrink simultaneously, forming a softer yet stronger finished product, and the film is safe, it contains no solvents, adhesives, and emits no vapors.  The material will maintain its properties under extreme temperatures and the unique laminating process allows the film to remain soft without altering the original characteristics of the inner and outer layers.  

AS+I is recyclable with certain recyclers, with the fibers adding strength to many recycling products.  FPM utilizes some ISO9000 certified suppliers
ArmorShield Plus InterceptTM and AS+ITM are trademarks of FPM Inc. www.shrinkwrapping.com & www.InterceptShrinkfilm.com, HQ: Flat Rock, MI.  For more information please contact Mr. Randy Dutton, 360-249-5833 P.S.T. InterceptShrinkfilm@gmail.com or our HQ at 800-222-4449, info@shrinkwrapping.com.   FPM is a service-connected, disable-veteran-owned, small business with ISO 9001:2000 and ISO 14001 certification.  AS+I is made in the US.
[image: image2.png]FPM

INCORPORATED




                                          [image: image3.png]\
‘/” ILRLEPT
-’



…simply better protection          
